| Element | Content |
| --- | --- |
| W | 75 – 78 |
| C | 0,20 max. |
| Cu | 0,15 max. |
| P | 0,05 max. |
| Sb | 0,05 max. |
| Si | 1,5 max. |
| Mn | 0,25 max. |
| S | 0,08 max. |
| As | 0,05 max. |
| Sn | 0,08 max. |

All our products shall be labelled with product name, reference number and net weight. Each delivery is accompanied by a certificate of analysis and the delivery note.

Size                                               Packaging

Delivery time                                Remarks

Ferro Tungsten

COMETAL, S.A.

• C/José Lázaro Galdiano 4

• 28036 Madrid (Spain)

• Ph:  +34 91 4585980

• Fax: +34 91 4585987

• cometal@cometalsa.com

• www.cometalsa.com

• VAT Nr ESA28117026

Your Door to Raw

Materials & Markets

Descripción

10 to 50 mm.

10 to 100 mm.

Drums with 250 Kg

Drums with 500.

Prompt.

Typical content (% w/w)